# PRODUCT DEFINITION SHEET

PRODUCT NAME: TECHCOAT G4S

CODE: G4S

PRODUCT DESCRIPTION: CONCAST MOULD PAINT

| CRITICAL PROPERTIES |  |  |
| --- | --- | --- |
| SPECIFICATION | SG | 11-15 |
| SOLIDS CONTENT |  | 21-32% |

| SUPPLEMENTARY PROPERTIES |  |  |  |
| --- | --- | --- | --- |
| CHEMICAL ANALYSIS % (DRIED SAMPLE) |  |  |  |
|  |  | RANGE | TYPICAL |
|  | CARBON | 17-27% | 22.79 |
|  | Na20 | 2% MAX | 0.29 |
|  | SiO2 | 6% MAX | 3.49 |
|  | Al203 | 2% MAX | 1.38 |
|  | H20 | 68-79% | 72% |

…………………………………………………..

###### For and on Behalf of Ace Coatings Ltd